## Slide 1: f
Performance of Concrete Incorporating
Super Absorbing Polymers
Mentor:- Dr. Sushree Sunayana
Presented by:- Khushi Kumawat (2022UCE1610)
Gaurav Singh (2022UCE1243)
Nigam Kumar (2022UCE1425)

## Slide 2
Introduction to SAP
Super Absorbent Polymer (SAP) are cross-linked polymers commonly composed of polyacrylate-based polymers capable of absorbing water several times their own weight.
When incorporated in concrete, SAP enables internal curing, especially beneficial for low w/c mixes.
SAP
Mechanism of SAP & Internal Curing
SAP absorbs water in its pre-wetted state during mixing and acts as an internal water reservoir.
As hydration progresses and internal relative humidity decreases, SAP gradually releases the stored water into the cement matrix.
This continuous water supply supports further hydration, reduces self-desiccation, and enables effective internal curing.
Swollen SAP

## Slide 3
Need of the study
Low water-cement ratio concrete often lacks sufficient internal moisture for complete hydration.
External curing becomes challenging in semi-arid regions or in hot climate.
This results in self-desiccation, early-age cracking, and reduction in strength.
Optimal dosage of SAP for low w/c concrete is still not well-established, despite the capability of SAP to act as internal water reservoirs.

## Slide 4
Objectives of the study
To investigate the absorption and desorption kinetics of Super-absorbing polymer in cementitious solution.
To investigate the effects of SAP on fresh and hardened concrete properties.
To determine the optimised dosage of SAP with a suitable low water-cement ratio.
To perform predictive analysis using statistical and machine learning models based on experimental data.

## Slide 5
Methodology
Study previous literatures and formulate objectives based on research gaps
Prepare concrete mixes with varying water-cement ratio with different SAP dosage
Experimental Testing
Fresh Concrete Property
Workability (Slump Test)
Hardened Concrete Property
Strength (Compressive Strength Test)
Data Analysis & Reporting
Data analysis and optimization
Literature Review
Mix Design
Preparation
Curing Comparison
Machine Learning and predictive modelling
Report writing and final presentation
4

## Slide 6
Literature Study
7
Sr. No. | Title | Author(s) | Year | Findings
1 | Superabsorbent Polymers for Internal Curing Concrete | Zhou, Wang, Taylor, Gu et al. | 2015 | Explains SAP chemistry and its role in internal curing; reduces self-desiccation, improves hydration, minimizes shrinkage, and enhances durability.
2 | Influence of Superabsorbent Polymers on the Surrounding Cement Paste | Wang, Yang, Hu, Li, Cheng et al. | 2016 | Shows SAP affects microstructure; increases early porosity but reduces it later; improves hydration (~5%) but may slightly reduce early strength.
3 | Application of SAP in Concrete Construction – RILEM Update | Mechtcherine, Wyrzykowski, Schrofl et al. | 2017 | Highlights shrinkage control, improved freeze–thaw resistance, and discusses challenges like SAP variability and dosage control.
4 | Measuring Absorption of SAP in Cementitious Environments | Zhao, Jensen, Hasholt | 2014 | Discusses testing methods like tea-bag method; absorption depends heavily on ionic concentration; emphasizes accurate measurement techniques.
5 | Absorption & Release Mechanism of SAP | Viktor Mechtcherine | 2010 | Explains swelling and desorption based on osmotic pressure and humidity gradients; polymer structure affects performance.
6 | Application of Super Absorbent Polymers (SAP) in Concrete | RILEM Technical Committee 225-SAP | 2013 | Provides guidelines on SAP use; covers rheology, shrinkage reduction, durability, and need for standardization.

## Slide 7
Objective 1
“To investigate the absorption and desorption kinetics of Super-absorbing polymer in cementitious solution.”
Absorption test
Desorption test
Tea-bag Absorption test
Open air-drying test
SAP Characteristic Property Tests:

## Slide 8: Tea-bag Absorption Test
pH value determination using probe:
  Distilled Water (D.W) = 7.2
  Tap Water (T.W) = 8.4
  Cement Filtrate (C.F) = 13
1, 5, 10, 30, 60 min, 3 and 24 h after the SAP/liquid contact, the tea-bag with swollen SAP was taken out, gently wiped with a dry gauze, and weighed (mass mTB3)
pH measuring probe

## Slide 9: Tea-bag Absorption Test Results
Absorption Capacity Curves
(This results shows average of the three trials)
Distilled Water
Tap Water
Cement Filtrate

## Slide 10: Tea-bag Absorption Test Results
Distilled Water
Tap Water
Comparing values upto 24 hr:

## Slide 11: Desorption Test
Open dry desorption in environmental conditions:
The Curve shows desorption rate of the SAP with number of days
Distilled Water
Tap Water
Whatman filter paper

## Slide 12: Inference:
SAP absorption-desorption behaviour:
Absorption:
  SAP absorbs highly in distilled water (380–420%), moderately in tap water (230–260%), and very poorly in cement filtrate (<60%).
  Therefore, SAP must be pre-wetted before adding to concrete.
Desorption:
  SAP releases water slowly at 7–13 gm/day, providing continuous moisture for several days.
  Distilled water SAP desorbs slightly more than tap-water SAP due to higher initial swelling.
Interpretation:
  This behaviour supports the internal curing mechanism: SAP provides internal curing water once the external curing might be insufficient, ensuring better hydration and reducing self-desiccation.

## Slide 13
Objective 2
“To investigate the effects of Super-absorbing polymer on fresh and hardened concrete properties.”

## Slide 14: Fresh Concrete Test Slump Test-
Tamping and measuring rod
Slump cone

## Slide 15: Fresh Concrete Test
Slump Test-
Composition Number | Water Cement Ratio | SAP Dosage (% of cement by wt) | Slump Value (mm)
1 | 0.4 | 0.2 | 70
2 | 0.4 | 0.4 | 150
3 | 0.4 | 0.6 | 200
4 | 0.45 | 0.2 | 170
5 | 0.45 | 0.4 | 230
6 | 0.45 | 0.6 | 300
7 | 0.38 | 0.2 | 70
8 | 0.38 | 0.4 | 100
9 | 0.38 | 0.6 | 190
10 | 0.36 | 0.2 | 10
11 | 0.36 | 0.4 | 40
12 | 0.36 | 0.6 | 70
13 | 0.34 | 0.2 | -
14 | 0.34 | 0.4 | 30
15 | 0.34 | 0.6 | 60
Effect of SAP dosage variations- SAP dosage Slump
Effect of water-cement ratio variations- w/c Slump
When used in pre-wet condition and in suitable dosage, SAP provides the required workability which we lack in concrete with low water cement ratio.
Inference:

## Slide 16: Hardened Concrete Test
Compressive Strength Test-

## Slide 17
Objective 3
“To determine the optimised dosage of SAP with a suitable low water-cement ratio.”

## Slide 18
7-Day Compressive Strength Test:

## Slide 19
7-Day Compressive Strength Test:
Inferences:
Best: w/c = 0.38 with 0.2 SAP
Excess SAP (0.6%) → reduces strength
Trend:
It will depend on the dosage and water–cement ratio; there is no general trend.
Optimum dosage lies between 0.2 and 0.4

## Slide 20
28-Day Compressive Strength Test:

## Slide 21
28-Day Compressive Strength Test:
Inferences:
At w/c = 0.40 → 0.2% SAP gives highest strength
At w/c = 0.36 → 0.4% SAP performs best
At w/c = 0.34 → higher SAP improves strength due to internal curing
Trend:
SAP effect increases as w/c decreases, meaning that SAP’s effect is greater in low w/c ratio concrete.

## Slide 22
Concrete Type | Avg. 7-Day Strength (MPa) | Avg. 28-Day Strength (MPa)
Without SAP | 27.8 | 29.2
With SAP (0.2%) | 23.8 | 32.1
Readings:
Inference:
At 7 days → Without SAP > With SAP
At 28 days → SAP mix shows comparable / higher strength
Trend:
Early age → SAP ↓ strength
Later age → SAP ↑ hydration → ↑ strength
Comparison of compressive strength with and without SAP
“To compare and analyse the strength of concrete with and without SAP.”

## Slide 23
Curing Mechanism | Avg. 7-Day Strength (MPa) | Avg. 28-Day Strength (MPa)
Conventional + Internal Curing | 19.8 | 26.6
Internal Curing (SAP) | 16.9 | 20.5
Readings:
Inference:
At 7 days → Conventional + Internal > Internal only
At 28 days → Combined curing gives the highest strength
Trend:
More curing water → better hydration → higher strength
“To compare internal curing and conventional curing and investigate their effects on concrete performance.”
Comparison of conventional curing and internal curing

## Slide 24
Objective 4
“To perform predictive analysis using statistical and machine learning models based on experimental data.”

## Slide 25
Problem Statement:
Concrete strength prediction is critical in construction
Traditional testing:
  Time-consuming (7, 14, 28 days)
  Costly and labour-intensive
Need for:
  Faster prediction
  Cost reduction
  Optimisation of materials
Goal: Predict compressive strength using ML instead of physical testing
Objective:
Develop an ML model to predict concrete strength
Analyze effect of:
  SAP %
  Water-Cement Ratio
  Age
Build:
  API (Flask)
  Frontend (Streamlit)
Provide:
  Real-time prediction
  Visualization + Explainability

## Slide 26
Dataset Description:

## Slide 27
Exploratory Data Analysis (EDA):

## Slide 28
Exploratory Data Analysis (EDA):

## Slide 29
Exploratory Data Analysis (EDA):

## Slide 30
Model Selection:
Algorithm Used:
  Gradient Boosting Regressor(Final Model)
Why XGBoost?
  Achieved the highest R² score (0.9144) indicating better prediction performance
  Produced the lowest RMSE (1.9901) showing minimum prediction error
  Obtained the lowest MAE (1.4265) ensuring more accurate predictions
  Handles non-linear relationships effectively
  Uses boosting (sequential learning) to improve model performance step-by-step
  Provides better generalization compared to other evaluated models

## Slide 32
Model Validation:
  Points are close to diagonal line
  Indicates good prediction accuracy
Error Analysis:
Gradient Boosting has:
Lowest error among all models
Confirms it as best performing model

## Slide 34: Deployment (Live System)
End-to-End ML system deployed using:
  Frontend: Streamlit
  Backend: Flask API
Features:
  Real-time prediction
  Interactive graphs
  Strength classification
🌐 Live Application Link
Your Deployed Link Here

## Slide 35: Conclusions
Pre-wetted SAP provides effective internal curing by storing and releasing water during hydration, as SAP shows effective absorption-desorption behaviour.
Workability: Slump improves with pre-wetted SAP due to additional available moisture
7-day strength: SAP mixes show slightly lower strength than the control mix.
28-day strength: SAP mixes show comparable or improved strength, especially at low w/c ratios.
Optimum SAP dosage: 0.2% - 0.4%
Recommended mix: w/c = 0.36 with 0.4% SAP (pre-wetted)
Overall: SAP improves workability and long-term strength, while excess SAP (0.6%) reduces strength due to void formation

## Slide 36
Timeline

## Slide 37
THANK YOU
37